## Slide 1
2D perovskite diffraction pattern simulation
Zihan Zhang

## Slide 2
An+1BnX3n+1 or R2An-1BnX3n+1
Self-assembled 2D material
Enhanced moisture stability
Anisotropic charge transport (Quantum well)
High exciton binding energy
Promising material for light-emitting diodes, spin valves, and field-effect transistors
Ruddlesden-Popper phase
isotropic
anisotropic

## Slide 3
Orientation:
Spin coating:
(PMA)2PbI4
(PPA)2PbI4

## Slide 4
Python Program for GIWAXS simulation:
https://github.com/ZihanZhang-1996/2D_diffraction
Input:
1.
2. crystal structure
Gaussian distribution model:
Single crystal: ,
Power diffraction: , ∞
2D material (isotropic in-plane, anisotropic out-of-plane): finite, ∞
Program
output:
Diffraction pattern
in qz ,qxy
(PMA)2PbI4
Python & matlab

## Slide 5
Algorithm:
1. Bragg peaks
Read crystal structure from POSCAR file
POSCAR ↔ CIF
By VESTA VASP …
where

## Slide 6
Algorithm:
1. Bragg peaks
Rotation Matrix
c
z
x
c
c
c
c
y
z
y
x
Rotate around y axis

## Slide 7
Algorithm:
1. Bragg peaks
Atomic Form Factor
AFF.py

## Slide 8
Algorithm:
Calculate the intensity:

## Slide 9
Examples:
Graphite single crystal:
, , in-plane(qx, qy)
Experiment:
2D perovskite GIWAXS
finite, , (qz, qxy)

## Slide 10
The model is not well-defined near qz:
and
is not independent at qxy=0.
This is not a serious problem because:
2D material (isotropic in-plane, anisotropic out-of-plane): finite, ∞
Missing wedge

## Slide 11
Input:
(hkl) dimension,
Wavelength λ, Rotation angles in x,y, Image grid
function
[lattice constants, atom positions]
= Read(POSCAR)
function
[Brag peaks]
= rcpeaks(crystal structure, (hkl) dimension, Rotation)
function
[Intensity]
=Intensity_Gaussian(Brag peaks, , , Image grid)
function
[Intensity]
=Lorentz_polarization_correction(Intensity, wavelength)
(qz,qxy) plane Image display
Runtime:
image = 500 x 500 pixels
(hkl) = from -5 to 5
< 1min on PC
https://github.com/ZihanZhang-1996/2D_diffraction